## Slide 1: The course is developed under Erasmus+ Program Key Action 2: Cooperation for innovation and the exchange of good practices Knowledge Alliance
TRAINING MODULE
FINISHING, PRINTNIG and FUNCTIONALIZATION
Course: Finishing in the Function of Textile Printing
Partner: P4 – University of Zagreb Faculty of Textile Technology
Prof. Martinia Glogar, Ph.D.
The information and views set out in this publication are those of the authors and do not necessarily reflect the official opinion of the European Union. Neither the European Union institutions and bodies nor any person acting on their behalf may be held responsible for the use which may be made of the information contained therein.
ICT IN TEXTILE AND CLOTHING HIGHER EDUCATION AND BUSINESS
Project Nr. 612248-EPP-1-2019-1-BG-EPPKA2-KA

## Slide 2
The information and views set out in this publication are those of the authors and do not necessarily reflect the official opinion of the European Union. Neither the European Union institutions and bodies nor any person acting on their behalf may be held responsible for the use which may be made of the information contained therein.

## Slide 3: MODULE – FINISHING, PRINTING AND FUNCTIONALIZATION
Course: Finishing in the Function of Digital Printing
Duration: 30 hours
Course objectives
ICT is a fundamental carrier of the development of digital printing in general and the transition of digital technology from graphic to textile printing. Digital printing allow to respond to market demands extremely quickly, with immediate and unique design personalization, and significant savings in water and energy. The aim of the course is to acquaint participants with the methodology of using ICT tools in designing and final printing process, to explain the basic features of the development of digital textile printing with emphasis on modern research trends in this field explaining the different types of textile pre-treatment in digital printing, such as plasma pre-treatment, chitosan pre-treatment, cationization, etc.
Topics
ICT as fundamental aspects of digital textile printing development - Current trends in the development of digital textile printing technology
Technical characteristics of digital textile printing - innovative approaches in the formulation of printing inks and modifications
Innovative approaches in digital printing pre-treatments processes
Learning outcomes
Knowledge | Skills | Responsibilities/autonomy
To know the complex interaction of heterogeneous textile structure and printing ink: concepts of deformation, penetration, porosity To understand the methods of pre-processing and post-processing of textiles as key stages in the application of the digital technology To understand the difference between dye-based and pigment-based printing inks and the difference in the mechanism of their bonding to textile materials To get acquainted with innovative methods of textiles pre-processing depending on the composition of the printing ink and the use of dyes or pigments | To use the ICT tools in designing and printing process To be able to handle a digital printing machine To identify and predict the interaction of textile material and printing ink depending on the structure and raw material composition To apply certain pre-treatment methods in dependence of textile material structure and composition To analyse the results of given pre-treatments To examine the difference in color and print quality with respect to the applied pre-treatment | To manage a digital printing device independently To take into consideration the environmental legislation related to the textile industry and the application of certain chemicals To apply responsibly pretreatment methods always considering the method with the least environmental impact To contribute to team work on setting the basic parameters of the printing process, pre-processing and post-processing of textiles

## Slide 4
MODUL: Finishing, Printing and Functionalization
Course: Finishing in the Function of Digital Printing
Course duration: 30 hours
Content: 4 units / 20 lessons
DESCRIPTION OF THE COURSE:
The course in Finishing in the Function of Digital Printing includes aspects of the transition of technology originally developed for the graphic industry to the field of textile printing. ICT itself is the foundation of the development of digital printing technology, which makes it an integral part of its application. However, due to the fact that digital technology has been developed for the graphic industry, which means printing on homogeneous surfaces, digital printing on textiles still faces many obstacles and unresolved issues that prevent its full commercialization.
Through this course, the mechanisms of interaction of printing ink droplets with specific surface structure of textile materials will be explained from the aspects of the technology and science, but from the aspect of design and creativity as well.
The basic directions of development will be presented, which include the development in the field of construction of the print head of a digital printing machine and the mechanism of droplet formation in Ink Jet technology, directions of development of the printing ink formulation and modifications and pre-treatments of textile materials.
Emphasis will be on novel trends and innovative solutions of textile pre-treatment, as well as up to date analysis methods, in the context of textile functionalization to achieve optimal print quality results.

## Slide 5
THE AIMS and OBJECTIVES OF THE COURSE:
The aim of the course is to acquire the skills and knowledge of digital textile printing, aiming in mastering the abilities of using the ICT tools in digital textile printing processes from designing phase to realization phase of, from the design phase to the realization phase, not only of the finished patterned textile material, but also of the complete garment.
In the course, applicants will be introduced to the most modern tools for testing certain properties crucial for the quality of digitally printed textiles, such as: SEM, MMT, FTT, DAS, spectrophotometry.

## Slide 6
UNIT 1 (5 LESSONS): Basics of Textile Printing
OVERWIE of:
ICT as the fundamentals of digital printing technology
Development and application of InkJet digital printing technology in textile printing
Technology of ink droplet formulation - characteristics and differences
Computer support in the design process, colour definitions, ink management, colour management
Right on time production, quick response to market demands, advantages and disadvantages of digital printing on textiles

## Slide 7
ICT as the fundamentals of digital printing technology
Development and application of InkJet digital printing technology in textile printing
The evolution and progress of digital printing of textiles, an overview of its development
Future perspectives – digital vs. conventional
Current state of industrial digital textile printing
comparison of conventional and digital printing from 2017.

## Slide 8
Technology of ink droplet formulation - characteristics and differences
Division of basic ink droplet formulation technologies
Technical characteristics of individual printing technology
Features of digital print commercialization
In the last decades numerous projects have been held in the field of InkJet textile printing technology with the basic aim of research – development of printing head as key factor in any InkJet printing process.
The important fact is that unique technology of ink flow formation still is not developed
Current trends in research and development of printing heads go in few parallel directions:
  Technology of continuous floe with binary deflection
  Technology of continuous flow with multiple deflection
  Technology of discontinuous flow (DOD) – thermal inkJet
  Technology of discontinuous flow (DOD) – piezoelectric InkJet
https://pubs.rsc.org/image/article/2020/CY/d0cy00040j/d0cy00040j-f1_hi-res.gif

## Slide 9
Computer support in the design process, colour definitions, ink management, colour management
Right on time production, quick response to market demands, advantages and disadvantages of digital printing on textiles
Historical overview (from 50-es till up to date development)
Industrial settings wit automation
Computer control settings
Print on demand
Print and cut
Advantages / Disadvantages
Quick response / complex interaction of ink with textile surface
Decrease of pre-printing costs / modification and adaptation of printing inks
Unlimited number of colors and pattern size / problem of textile porosity
Minimized production errors / equipment technical requirements
Optimal consumption of printing pastes / optimization of textile pretreatment and finishing phase

## Slide 10
RIP - Raster Image Processor
A raster image processor (RIP) is a software that translates (rasterizes) computer vector files (InDesign, Illustrator, Photoshop, PDF, JPG, etc.) to a raster image also known as bitmap that is composed out of a matrix of dots that the printer can understand and print. The raster image is similar to the pixels on the computer screen. The RIP software processes multiple content types for a specific print environment and communicates that processed data to the printer for final output.

## Slide 11
COLORGATE PROFESSIONAL RIP
Color matching accuracy, color library and matching with color atlases
Different image format support
Auto-adjustment of white base under semi-transparent areas
Advanced profiling and linearization tools
CALDERA TextilePro RIP
Color management
RGB Workflow
Color books and color atlases
Production optimization
Print & Cut

## Slide 12
UNIT 2 (5 LESSONS): Specifics of Digital Printing on Textiles
The influence of surface structural characteristics of textile materials on the formed shape, degree of deformation and spreading of the droplets on the surface of textile materials and penetration of printing ink droplets into the structure of textiles.
Mechanism of complex behaviour of ink jet inks due to the topological nature of woven/knitted textile fabrics and the adsorption behaviour of colorants on different textile fibres.
The image fomation in dependency on the physico-chemical ink properties, modeling of ink spreading and penetration.
Problems of modification and adaptation of inks and components of printing pastes for application in ink jet technology on textile.
The main streams in printing ink formulation development of printing - development of pigment based inks and binders; development of dye-based printing inks including dye modification, primarily reactive dyes, given the percentage of cellulosic materials being printed on a global market.

## Slide 13
….As much as the modelling of ink penetration and ink spreading, and their effect on print performance of paper have been well studied, these findings are still not verified for textiles where more complex behaviour of ink jet inks is anticipated due to the topological nature of woven/knitted textile fabrics, the diversity of colorants (dyes and pigments) and their adsorption behaviour on different textile fibres……..
A specific problem is the porosity of the textile material, which causes a certain loss of information in the reproduction, since the penetration of printing ink into the deeper layers of the textile substrate as well as the loss of printing ink on porous parts cannot be prevented.

## Slide 14
CURRENT RESEARCH DIRECTIONS
Printing ink formulation
Pigment based inks
Surface pre-treatment
Nano-scale binder development
Dye-based printing inks
Dyes modifications
Compared to dyes, the incorporation of pigments into ink jet inks is a much more difficult task. The pigments must be ground into very fine particles of 200 nanometers or less so that they will remain suspended in the ink and be transparent to light. Also, a pigment dispersion system must be provided to avoid flocculation which can cause the clogging of the ink jet print-head.
Nano-scale emulsions containing the mixture of soft and hard monomers in ration 8:1, employing butyl acrylate soft monomers, methyl methacrylate hard monomers, N-methylolacrylamide as crosslinking agents and monododecyl maleate as copolymerizable surfactant.

## Slide 15
UNIT 3 (5 LESSONS): Functionalization and Pre-treatment of Textiles in Digital Textile Printing
Up to date researches and aspects of innovative approaches in modifications and pre-treatments of textile materials.
Different pre-treatment methods (e.g. cationization, chitosan treatment, plasma treatment).
Preparation and processing of pre-treatment
When the printing ink touches the surface of the textile material, penetration and spreading occur. The ratio and specific relationship of penetration and spreading will depend on physical characteristic of the substrate surface and on the pre-treatment of substrate.
The function of fabric surface pretreatment is to immobilize the ink drop jetted onto the fabric to prevent its bleeding. So, chiotsan pretreatment, plasma technology and cationic compounds have been used to pretreat the fabrics.

## Slide 16
The purpose of cationic pretreatment of cotton is to improve printability with pigment by introducing positively charged sites on cotton. Due to the dye molecules in the ink drop being ionized, the ink drops are negatively charged. Therefore, the ink drops could be immobilized on the cationized fabric surface.

## Slide 17
SEM analysis of CO knit samples after: (a) untreated - without print (left)/ print (right) 1000x-2000x; (b) oxygen pretreated (left)/ print (right) 2000x; (c) argon pretreated (left)/ print (right) 4000x.
Compared with conventional techniques, plasma treatment has many advantages. Aspect of plasma-based surface treatment depends largely on the different effects which could be imparted to the fabric when using different gases to produce the plasma.

## Slide 18
UNIT 4 (5 LESSONS): Testing and Analysis
Colour objectification and spectrophotometric analyses, computer data analyses, computer colour and texture visualization
Characterization of non-treated and treated surface as well as ink droplet behaviour (scanning electron microscopy-SEM, moisture management analyses-MMT, drop shape analysis-DAS, pH measurement, hydrophilicity/ hydrophobicity of textile analyses, fabric touch testing-FTT).
Data analyses and numerical/graphical presentation, examples of results discussion.

## Slide 19
https://www.datacolor.com/business-solutions/product-overview/datacolor-envision/
Display colors accurately on a calibrated monitor, represented on multiple substrates
Metamerism evaluation
Color applied to textured substrates or full garment to replicate the visual experience
The possibility of creating mew substrates or garment, created using scanner or a digital camera

## Slide 20
Print on-demand manufacturing solution, for micro factory sample production, custom graphics or logos, efficient alignment of complex graphics, tailored.

## Slide 21
Characterization of non-treated and treated surface as well as ink droplet behaviour (scanning electron microscopy-SEM, moisture management analyses-MMT, drop shape analysis-DAS, pH measurement, hydrophilicity / hydrophobicity of textile analyses, fabric touch testing-FTT).
Moisture management tester
Drop shape analyzer

## Slide 22
Characterization of non-treated and treated surface as well as ink droplet behaviour (scanning electron microscopy-SEM, moisture management analyses-MMT, drop shape analysis-DAS, pH measurement, hydrophilicity/ hydrophobicity of textile analyses, fabric touch testing-FTT).
SEM images of non coated cotton (left) and cotton coated with acrylate binder with layer of pigment (right)
SEM images of non treated cotton (left) and cationized cotton (right)

## Slide 23
Characterization of non-treated and treated surface as well as ink droplet behaviour (scanning electron microscopy-SEM, moisture management analyses-MMT, drop shape analysis-DAS, pH measurement, hydrophilicity/ hydrophobicity of textile analyses, fabric touch testing-FTT).
The fabric touch tester simultaneously measures the fabric thickness, compression, bending, roughness, friction, as well as the thermal properties of the fabrics, thus objectively measuring the subjective properties of the fabric touch. The comprehensive, sophisticated design of the FTT allows it to measure all the mechanical and surface properties of fabrics in one simple test, and these are smoothness, softness, warmth, the overall feeling of hand touch.

## Slide 24
Coordinator:
Technical University of Sofia
Department of Textile Engineering
Project Manager of ICT-TEX:
Prof. ANGEL TERZIEV, PhD
е-mail: aterziev@tu-sofia.bg
Web-site: ICT-TEX.eu
CONTACTS
The information and views set out in this publication are those of the authors and do not necessarily reflect the official opinion of the European Union. Neither the European Union institutions and bodies nor any person acting on their behalf may be held responsible for the use which may be made of the information contained therein.